## Slide 1: Surface Evolution of Nb(100) due to Thermal/Gas Treatments as applied to SRF Cavities
A. Dangwal Pandey, G. D. L. Semione, C. Bate, S. Kulkarni, T. Keller, H. Noei, V. Vonk, J. Schaffran, M. Wenskat, D. Reschke, H. Weise, and A. Stierle
Review and recent results at DESY
MML
From Matter to
Materials and Life

## Slide 2: Superconducting radio frequency (SRF) Nb cavities
Why??
Higher efficiency of the cavities directly reduce the cryogenic load
  Realization of the continuous wave operation of European-XFEL
  Cost reduction in large future projects, International linear collider (ILC) (approx. 17000 cavities)
Goal: - attain higher efficiency (Q), and max. Eacc
Toperating = 2 K, Nb: Tc= 9.3 K,
Notes: EP mixture of 1 volume part HF (48 %) and 9 volume parts H2SO4 (96 % - 98 %)
Why CW? - For synchrotron like experiments profiting from high coherence and intensity

## Slide 3: Why do specific surface treatments lead to substantial changes in SRF cavity performance?
  Final thermal treatment of SRF Nb cavities, reviewed here:
Low-T bake: @120 °C (48 hrs)
N-infusion: 800 °C (3 hrs) + @120 °C (48 hrs) in N2
  RF penetration depth lies within top 100 nm
A systematic investigation of Nb surface is needed
to understand the physics behind these processes,
to recognize the key parameters in surface treatments
  A ‘reproducible’ recipe for Nb surface preparation
  Any change must happen at the surface.

## Slide 4: Extensive Nb sample R&D worldwide
Towards cavities with highest quality factors (at high gradients)
  Surface study of Nb with atomic details
Commonly used characterization methods:
Microscopy: secondary electron microscopy (SEM),
      transmission electron microscopy (TEM),
        atomic force microscopy (AFM) etc.
Spectroscopy: x-ray photo e spectroscopy (XPS),
secondary-ion mass spectroscopy (SIMS)
positron annihilation spectroscopy (PAS) etc.
Diffraction: grazing incidence x-ray diffraction (GIXRD),
        nano electron diffraction (NED) etc.
  Different strategies:
  Ex-situ characterization: investigation after surface treatment
Cavity cut-outs
Samples treated with cavities
Samples treated similar to cavities
  In-situ experiments: investigation during surface treatment
  Samples treated similar to cavities

## Slide 5: Extensive Nb sample R&D worldwide
Review of results reported from different labs within last 4 years
  Nb samples investigated:
  Thermal treatments
  N-treatments
  Nb-carbide precipitates and grain boundary segregation

## Slide 6: Surface evolution of Nb(100) in UHV @ DESY
Low -T bake at 120 °C as applied to superconducting RF cavities
In-situ surface monitoring using XPS:
Nb(100) model system of ultra-pure single crystal and cavity-grade material
120°C bake:
  Dissolution of Nb2O5,
  growth of NbO2 and NbO,
  stable surface achieved after 12 hrs baking
  Longer cavity baking of 48 hrs can be shortened
Nb2O5, NbO2, NbO, NbxO, Nb
120 °C
15 hrs
120° C
12hrs
120°C
2 hrs
RT
M. Delheusy, et al., Appl. Phys. Lett . 92, (2008)

## Slide 7: Extensive Nb sample R&D worldwide
Review of results reported from different labs within last 4 years
  Nb samples investigated:
  Thermal treatments
  N-treatments
  Nb-carbide precipitates

## Slide 8: Cut-outs of several cavities @ FNAL
TEM, SIMS, Cryo-AFM: identified NbH phases, confirmation of ‘N’ at metal-oxide interface, nanohydride segregation
Secondary Ion Mass Spectroscopy (SIMS):
- A. Romenenko, TTC meeting Riken Japan 2018
‘N’ present in N-infused Nb – N interstitials favorably trap H – suppress NbH segregation and thus suppress HFQS
Y. Trenikhina et al, J. Appl. Phys. 117,154507(2015)
Nb
oxide
TEM SAED
Electro polished (EP) Nb
Protective layer
A. Romanenko et al., IPAC 2018
M. Checchin et al., IPAC 2018
[A. Grassellino talk this session]
800°C/3hrs + 120°C in 25 mTorr (0.03 mbar) N2 /48hrs

## Slide 9: N-infusion at varying T @ Jlab
Fine grain Nb samples treated similar to cavities: XPS/SIMS/AC susceptibility measurements, ‘N’ containing phase
SIMS
XPS
800°C/3hrs + inject N2 @290°C + 120-160°C in 25 mTorr N2 /48hrs
P. Dhakal et al. Phys Rev. Accel and Beams 21 (2018)
a new chemical component observed, N excess within top 50 nm,
in-line with level of dirtiness observed by AC susceptibility measurements
Nb oxy-nitrate phase present on Nb surface after 140°C -160°C N-infusion
[P. Dhakal talk SRF2019]

## Slide 10: 160°C N-infusion @ Cornell
Large grain Nb samples treated with cavities: SIMS, interstitials diffuse in to lattice, much higher C compared to N
800°C/5h + 160°C/48hrs in 40mTorr N2 + 160°C bake 168 hrs
P. N. Koufalis, M. Liepe, J. T. Maniscalco, TUXBA01, SRF2017.
‘N’ observed only in top 5 nm, much higher C conc. in near-surface region
SIMS
160 °C low- T dope
[J. T. Maniscalco talk SRF2019]

## Slide 11: N-infusion of fine-grain Nb at varying T @ DESY
SEM: carbon rich precipitates for N-infused samples at 120 °C and 160 °C
XPS: more Nb-C content for infusion @ 160 °C, no Nb-N bonding observed
SIMS: more C for 160 °C infusion, no NbN identified
Samples treated with cavities: SIMS/ SEM/ XPS, more carbides on 160°C infusion, no indication of NbN
10 µm
N 1s
Nb-N
Higher carbide content for N-infusion at higher T to be related to failed cavity treatment
XPS
Nb 3d
C 1s
Nb-C
NbC
NbO
Nb2O5
160 °C N-inf.
120 °C N-inf.
160 °C N-inf.
120 °C N-inf.
Nb-N
800°C/3 hrs + 120°C/25 m Torr N2/ 48hrs ■
800°C/3 hrs + 160°C/25 m Torr N2/48hrs ▲

## Slide 12: N-infusion of Nb(100) in FNAL, investigation @ DESY
baseline
after N-infusion
Q0
SEM/XPS, shallow NbC precipitates, absence of Nb-N
Sample corresponding to a successfully infused cavity:
C-precipitates visible
No signature of ‘N’ containing phase
Nb-C
XPS
NbO
Nb2O5
Nb 3d
N 1s
C 1s
NbO2
NbxO
800°C/3hrs + 120°C in 25 mTorr N2 /48hrs
SIMS

## Slide 13: N-infusion of Nb(100) in UHV chamber @ DESY
in-situ XPS experiment
800 °C + 120°C/12 hrs in UHV (no N2)
NbO, NbC present on surface
No Nb-N observed

## Slide 14: N-infusion of Nb(100) in UHV chamber @ DESY
800 °C + 120°C/12 hrs in UHV (no N2)
+ 120 °C in N2 (0.004 m Torr)/13 hrs
NbO grows further
NbC still visible
Nb-N observed in top 10 nm surface
NbO, NbC present on surface
No Nb-N observed
in-situ XPS experiment, Nb-N observed

## Slide 15: N-infusion of Nb(100) in UHV chamber @ DESY
@ 500°C heated in UHV to remove N
+ 260°C 12 hrs
+ 260°C in N2 (0.004 mTorr)/15 hrs
Nb-N peak got intense by
N-infusion at 260 °C
397.3 eV
800 °C + 120°C/12 hrs in UHV (no N2)
+ 120 °C in N2 (0.004 m Torr)/13 hrs
NbO grows further
NbC still visible
Nb-N observed in top 10 nm surface
NbO, NbC present on surface
No Nb-N observed
in-situ XPS experiment, Nb-N observed

## Slide 16: N-infusion at very low N2 pressure @ DESY
Nb (100) sample: in-situ XPS experiment, Nb-N observed
@ 500°C heated in UHV to remove N
+ 260°C 12 hrs
+ 260°C in N2 (0.004 mTorr)/14 hrs
Nb-N peak got intense by
N-infusion at 260 °C
In-situ XPS:
Fully covered surface oxide layer suppresses signals from material underneath in earlier XPS investigations performed ex-situ.
Clear indication of NbN phase formed in 0.004 mTorr N2 partial pressure at 120°C
no peak at binding energy position for Nb-N bond
800 °C + 120°C/12 hrs in UHV (no N2)
+ 120 °C in N2 (0.004 m Torr)/13 hrs
formation of Nb-N phase within top 10 nm surface by N-infusion at 120 °C
397.3 eV
N 1s
A. Dangwal Pandey et al.,
J Material Science (2018) 53:10411
NbN
NbON
NbN: formed by nitridation of fine-grain Nb @ 900°C,
Oxidized in air for few months.
260°C in 0.004 m Torr N2
900°C N-doped
800°C N-doped
initial
120°C in 0.004 m Torr N2
A. Darlinski, Halbritter,
surface and interface analysis (1987) 10:223
NbN: formed by nitridation of large grain Nb @ 620°C,
Oxidized in air for 30 min.

## Slide 17: Extensive Nb sample R&D worldwide
Review of results reported from different labs within last 4 years
  Nb samples investigated:
  Thermal treatments
  N-treatments
  Nb-carbide precipitates/ grain boundary segregation

## Slide 18: Cavity cut-outs @ DESY: case study of failed runs
EBSD: Carbide segregation and grain boundary segregation
EBSD confirmed excessive grain-boundary segregation and precipitation of Nb2C
(111)
(001)

## Slide 19: Carbon-rich precipitates on cavity related samples
Nb
O
Larger and deeper saw-tooth like precipitates on heavily deteriorated cavities
Nb2C phase confirmed
Posiible sources of C: surrounding environment, dirty furnace etc,
Cavity improved after N-infusion @FNAL
Still good cavity performance after heat treatment 800 °C +120°C @DESY
Highly deteriorated cavity after heat treatment 800 °C +120°C @DESY
C
N
O
C
O
C
N
N
FIB lamella, Energy dispersive x-ray analysis, Electron backscatter diffraction (EBSD)
1DE20 large grain Nb
Baseline test at DESY (2007)
Test at FNAL after N-infusion (2019)
Notes: Electron backscatter diffraction (EBSD) is a Scanning Electron Microscope based microstructural-crystallographic characterisation technique

## Slide 20
Review of Nb surface analysis after thermal /gas treatments by in-situ and ex-situ methods
N-infusion: contradictory findings on presence of Nb-N from different labs by ex-situ meas.
  NbN signal reported by FNAL (20 nm), Jlab (50 nm), Cornell (5 nm) using SIMS,
  could not be observed by KEK and DESY in ex-situ XPS and SIMS, and in-situ XRD experiments
  BUT… different experimental conditions, different infusion recipes, and different Nb material
Confirmation of N bound to Nb after 120°C N-infusion at low pressure by in-situ XPS
  N2 partial pressure three orders of magnitude lower than that used for cavities
  Nb-N is formed at the interface ? role of N?
Low-T bake @ 120 C without Nitrogen
  Dissolution of Nb2O5, growth of NbO2 and NbO,
  stable surface achieved after 12 hrs baking compared to 48 hrs long baking time for cavities
Carbide segregation on decayed cavities
  Observed on samples treated with cavities as well as on cavity cut-outs
  larger and deeper precipitates <-> worse cavity performance
  Excessive Nb2C segregation at grain boundaries confirmed for lossy area of cavities
Clean conditions necessary for suppression of carbides!
Summary:

## Slide 21: Acknowledgements
Colleagues at Cornell, FNAL, Jlab, KEK for the collaboration
BEEM (electron microscopy) group at TUHH
DESY Nanolab team and MSL/MPL group at DESY
Thank you very much for your attention!

## Slide 22: N-doped Nb single crystals @ DESY
N-doped Nb @ 800°c , 900°C
Nb2O5
NbO2
NbO
Nb
A. Dangwal Pandey et al., J Material Science (2018) 53:10411–10422
N 1s
Nb-N
Nb(100) treated similar to cavities: ex-situ SEM/EDX/ XPS
XRD
XPS
AFM
SEM
EDX
800°c
900°c
Notes: X-ray photoelectron spectroscopy , Our observation:
NbN : 203.8 eV, NbC : 203.3 eV, NbO: 204.0 eV

## Slide 23: Surface evolution of Nb
during thermal and gas treatments as applied to superconducting RF cavities
My research
To investigate key surface properties related to significant improvements in cavity performance after particular treatments
Nb(100) model system of ultra-pure single crystal and cavity-grade material
In-situ surface monitoring using XPS:
120°C bake: Dissolution of Nb2O5, growth of NbO2 > NbO, stable surface achieved after 12 hrs baking compared to 48 hrs long baking time for cavities
N-infusion: direct observation of Nb-N bond formation pointing to possible ‚role of nitrogen‘ in better cavity performance.
I. Low -T bake at 120 °C:
Nb2O5, NbO2, NbO, NbxO, Nb
II. N-infusion :
800 °C +120°C/12 hrs (no N2)
+ 120 °C in N2 (5e-6 m bar)/13 hrs
120 °C
15 hrs
120° C
12hrs
120°C
2 hrs
RT

## Slide 24: Bulk Niobium: Specification for European XFEL cavities
Technical specifications of niobium applied to the fabrication of 1.3 GHz superconducting cavities for the XFEL
ASTM 6
(residual resistivity ratio)

## Slide 25
XPS of NbN
A. Darlinski, Halbritter, surface and interface analysis (1987) 10:223
Notes: X-ray photoelectron spectroscopy , Our observation:
NbN : 203.8 eV, NbC : 203.3 eV, NbO: 204.0 eV

## Slide 26: Cavity cut-outs:
2nd sound measurements and temperature maps of 1DE 16
Hot-spots from T-maps @ 1.5 K and 2 K
Quench-spot from 2nd sound
Samples measured at Nanolab:

## Slide 27: Cavity cut-outs @ DESY:
Case study of a failed infusion : XPS
2 µm
Cold spot
Hot spot
202.7 eV
Quench spot
Nb-C
Nb-O
Nb 3d
C 1s
O 1s
[Arti Dangwal Pandey]
Cavity treatment: 800°C 3 hrs + 120°C 48 hrs
NbxO/ NbxC ?
Defective oxide interface

## Slide 28: Cavity cut-outs @ DESY
Quench spot
Cold spot
Cavity treatment: 800°C 3 hrs + 120°C 48 hrs
Case study of a failed infusion– SEM/SIMS/EBSD - Nb-carbide precipitates
2 µm
2 µm
Hot spots and quench spots:
SEM: Niobium Carbides are denser and larger
SIMS: higher Carbon-Signal in the first ~20nm
Size and density of carbides detrimental for RF performance