## Slide 1: A promising approach for monolithic integration of III-V semiconductors on Si
NANOHETEROEPITAXY
METHODOLOGY
RESULTS
CONCLUSION
Anagha Kamath, and Fariba Hatami Institut für Physik, Humboldt-Universität zu Berlin, Newtonstrasse 15, 12489 Berlin, Germany Oliver Skibitzki Innovations for High Performance Microelectronics, Im Technologiepark 25, 15236 Frankfurt (Oder)
We present a distinctive approach “nanoheteroepitaxy”, to monolithically grow high quality, defect free III-V semiconductors (InP and GaP) on arrays of Silicon nanotips (Si NT’s) embedded in SiO2 matrix using Gas Source Molecular Beam Epitaxy (GS-MBE).
Fabrication of Si NT embedded in SiO2 matrix at IHP
SiO2:Si etching in 5 ml of 0.5% HF solution and 500 ml distilled water for 17 s
Prebaking the sample in the intro-chamber of MBE system
Epitaxial growth of III-V semiconductor on Si NT
Desorption (oxide-off) process in the growth-chamber of MBE system at T= 750o C for 15 mins
ACKNOWLEDGEMENT
This research project is supported by German Research Society (DFG) and DAAD Research Grant.
The SEM measurements were performed by
Christian Golz, M.Sc., HU Berlin.
SEM result of the array of Si NT with 0.5 µm × 0.5 µm pitch distance embedded in SiO2 matrix.
The SiO2 : Si etching conditions have been optimized for growth.
The selective growth of III-V semiconductors on Si NT’s still needs to be accomplished.
MOTIVATION
Line scans of single Si NT for different etching time
AFM images of single Si NT indicating its exposed height with etching time t= 20 s
Growth of GaP on the substrate with TG= 558o C, ØPH3= 3 sscm and growth rate 0.3 ML/s
Growth of InP on the substrate with TG = 500o C, ØPH3= 3 sscm and growth rate 0.3 ML/s